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          Specification
Customer Name：                               
客户名称：
Customer P/N:                                
客户品号：
Factory P/N：       GNL-2835UBC          
公司品号：

Description：                                   

产品名称
[image: image5.jpg]GN‘O"R

Lighting
LED TECHNOLOGY



                                        G-Nor Optoelectronics Co.,Limited.

Add:  No.81 YiFu Road, ZhuangShi

  Zhenhai, 315201,Ningbo, China.

Tel:  86-574-87503097, 87502706

Fax:  86-574-87503457
Website: http://www.g-nor.com
Client approval

客户审核

Wenliang  approval

基洛光电审核

Confirmation

制作

Approval

核准

Audit

确认

Confirmation

制作

Approval

核准

Audit

确认

□ Qualified        □ Disqualified

接受                不接受

DATE：
日期 ：

注：1.此规格书以中英文方式书写,若有冲突以中文版本为准文本.

2.此规格书的最终解释权归深圳稳亮电子股份有限公司

3.承认签章后请回复一份（或复印件）给我公司，其余由贵司留作存盘。如果在签章的承认书（或复印件）回复我司之前，下了有关此零件的订单且又无特殊说明，那么我司就确定贵司已完全承认。

      Please return one specification or one copy of it with your chop and signature of approval and retain the others for your record.In the event of an order being placed for this part number before the chop and signed with specification (or copy) is returnde and without special explanation,it will be assumed that full approval have been given.
TYPE NO:  GNL-2835UBC
PACKAGE  DIMENSIONS （产品尺寸）
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Notes:（备注）
1. All Dimensions are in millimeters （所有尺寸都以毫米为单位）
2. Tolerance is ±0.1mm Unless otherwise specified.（公差为±0.1mm，除非另有规定）
Device Selection Guide（选择指南）
Emitting Color（发光颜色）
Lens Type（胶体类型）
              Blue  蓝
Transparent  透明
Absolute Maximum Ratings at Ta=25℃（绝对最大额定值）
Parameter（参数）
Symbol（符号）
Rating（值）
Unit（单位）
Power Dissipation（功耗）
Pd

180
mW

Peak Forward Current[4]（峰值电流）
IFP

90
mA

Forward Current（正向电流）
IF

60
mA

Reverse Voltage（反向电压）
VR

5

V

Operating Temperature（操作温度）
Topr
-40℃ to+100℃
Storage Temperature （保存温度）
Tstg
-40℃ to+110℃
Lead Soldering Temperature

【3mm From Body】（焊接温度）
Tsol
260℃ For 5 Seconds

Electrical Optical Characteristics at Ta=25℃（电性与光学特性）
Parameter（参数）
Symbol（符号）
Min （最小）
Typ （平均）
Max（最大）
Unit（单位）
Condition （测试条件）
Forward Voltage（正向电压）
VF
2.8

3.0
3.2
V

IF=60mA

Luminous Intensity（亮度）
IV
3
--
5

LM

IF=60mA
Peak wavelength （峰值波长）
λp

--

--
--

nm

IF=60mA
Dominant wavelength（主波长）
λd
460
--
465
nm
IF=60mA

Reverse Current（反向电流）
IR
/

/

5

μA

VR=5V

Viewing Angle（角度）
2θ1/2

/

120

/

deg

IF=60mA

Notes.（备注）

1.The above luminous flux measurement allowance tolerance is±11%.（上述发光通量的测试允许公差为±11%）2.The above dominant wavelength measurement allowance tolerance is±1NM（以上所示波长测量误差±0.1V.）
3.The above forward voltage measurement allowance tolerance is ±0.1V. （以上所示电压测量误差±0.1V.）
4.1/10 Duty cycle, 0.1ms pulse width.（脉宽0.1ms,周期1/10）
Typical Electro-Optical Characteristics Curves（典型电光特性曲线）
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Soldering condition （焊接条件）
Reflow Soldering （回流焊接）
Hand Soldering（手工焊）
Lead Solder   （铅焊料）
Lead – free Solder（无铅焊料）
Pre-heat（预热温度）
120~150℃
180~200℃
Temperature
350℃ Max.

Pre-heat time（预热时间）
120sec. Max.

120sec. Max.

Soldering time

3sec. Max.

(one time only)

Peak temperature（峰值温度）
240℃ Max.

260℃ Max.

Soldering time （焊接时间）
10sec. Max.

10sec. Max.

Condition（状态）
refer to

Temperature-

Profile 1

refer to

Temperature-

Profile 2
Temperature profile in re-flow machine for lead type and lead free type（铅型和无铅型回流机的温度分布图）
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Dimension of carrier tape（载带尺寸）
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Dimension of reel（卷盘尺寸）
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Notes:（备注）
All dimensions are in mm, tolerance is±2.0mm unless otherwise noted.

（ 所有尺寸均为毫米，公差为±2.0mm，除非另有说明。）
Specifications are subject to change without notice.
    （规格如有更改，恕不另行通知。）
Packing（包装）
4000 piece of SMD 2835 Products on one reel. The reel will be put in the anti-static bag, then sealed.

（4000片SMD 2835产品在一个卷筒上。卷筒将放在防静电袋中，然后密封.）
4000 piece of SMD 2835 products on one bag.

  （4000件SMD 2835产品在一个袋子上。）
注意事项：
通过使用适当的工具从材料侧面夹取，不可直接用手或尖锐金属压胶体表面，它可能会损坏内部电路

Through the use of appropriate tools from the material side of the clip, can not be directly used by hand or sharp metal pressure on the surface, it may damage the internal circuit
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SMD吸咀外径不可超过LED尺寸，吸咀内役尺寸应尽可能大，吸咀顶端材质建议采用柔软材料以防在吸取期间刮伤或损坏LED胶体表面，元件的尺寸必须在取放机里准备的编程好，以确保精确的吸取和避免生产过中的损害

SMD suction nozzle diameter can not exceed the size of LED, the 

suction mouth battle size should be as large as possible, ceiling tip

 top material suggestions made of soft material to prevent absorb 

during scraping injury or damage the LED colloid surface, the size 

of the components must be in good pick and place machine to 

programming to ensure accurate absorption and avoid damage in 

production
                    
不可将模组材料堆积在一起，它可能会损坏内部电路            4.  不可用在PH<7的酸性场所
Do not stack together assembled PCBs containing            Not suitable to operate in       LEDs. Impact may scratch the silicone lens or damage                 acidic envi-ronment，PH<7

the internal circuitry
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5.  LED工作环境与LED适配的材料中硫元素及化合物不可超过100PPM

LED working environment is very suitable for the materials of LED and sulfur elements and compounds can not be more than 100PPM

当我们需要使用外封胶涂抹LED产品时，应确保外封胶与LED封胶胶水相匹配，因为大多数LED的封装胶水为硅胶，它有较强的的氧化性和较强的吸湿性.必须防止外封材质进入LED内部以造成LED的损伤，单一的溴元素含量要求小于900PPM，单一氯元素含量要求小于900PPM，在涂抹LED产品时要求外封胶溴元素与氯元素总含量必须小于1500PPM
When we need to use external glue for LED application products, please make sure that the exter- nal glue matches the LED packaging glue. Additionally ,as most of LED packaging glue is silica gel, and it has strong Oxygen permeability as well as strong moisture permeability; in order to prevent ex- ternal material from getting into the inside of LED, which may cause the malfunction of LED, the single content of Bromine element is required to be less than 900PPM,the single content of Chlorine element is required to be less than 900PPM,the total content of Bromine element and Chlorine element in the external glue of the application products is required to be less than 1500PPM

在密闭、高温的环境中，灯具内可能含硫/氯/溴等物质，这些硫、氯和溴元素会挥发成气体并腐蚀 LED 光源。因为 LED 封密硅胶具有多孔性结构，与光源镀银层发生硫化反应。LED 光源出现硫化反应后，产品功能区会黑化，光通量会逐渐下降直至微亮，色温出现明显漂移，LED 光源最终会失效。

建议您进行灯具排硫测试，确保 LED 光源在无硫/氯/溴等物质环境进行工作。

如出现硫化、氯化、溴化等造成的灯具异常，我司不承担此异常造成的损失。
In a closed, high-temperature environment, the lamp may contain sulfur / chlorine / bromine, andthese elements will evaporate into gas and corrode the LED light source. Because LED sealing silica gel has porous structure, sulphization reacts with the light source silver plating layer. After the vulcanization reaction of the LED light source, the product function area will be blackened, the light flux will gradually decline until slightly bright, the color temperature will drift significantly, and the LED light source will eventually fail.

It is recommended that you conduct lamp sulfur removal test to ensure that LED sources work in sulfur / chlorine / bromine.

For abnormal lamps caused by sulfide, chlorination and bromide, we will not bear the loss caused by this abnormality.

 本产品不可在以下条件下使用，如果产品在以下条件下使用，评估其使用效果和风险是有必要的：

-直接或间接的打湿或受潮，比如淋雨等；

-被海水损害或侵蚀；

-被暴露于腐蚀性气体(如 Cl2,H2S、NH3、SOx、NOx 等)；

-被暴露于粉尘、液体或油；

上述原因都会引起硅胶劣质化（如发黑、变色、开裂等）

This product may not be used under the following conditions, and it is necessary to assess its use effectiveness and risk if it is used under:

-Direct or indirectly wet or damp, such as raining rain;

-Damaged or eroded by seawater;

-Exposed to corrosive gases (e. g. Cl2, H2S, NH3, SOx, NOx, etc.);

-Exposed to dust, liquid, or oil;

The above causes will cause silicone deterioration (such as blackening, discoloration, cracking, etc.)

在开包装之前，请先检查包装袋有无漏气，如有漏气现象，请退回我司重新除湿包装再使用。

Before opening the package, please check the packing bag is free of leakage, if there is leakage phenomenon, please return the division to re - use the packaging and re - use
要在规定环境条件中使用：温度30℃以内，湿度60%RH以下

  To be used in the provisions of the environmental conditions

折包使用前：请用70℃除湿24小时后才可以使用

Please use 70 degrees 24 hours before you can use the10 after the use of the material is more than 24H of the use of time is not used up

材料拆装后使用时间超过24H未用完，需烘烤70℃/24小时除湿才可使用。

Need to bake 70 degrees /24 hours before the use of the desiccant can be used


G-NOR OPTOELECTRONICS CO.,LTD.
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